DECLARATION OF CONFORMITY:
	                                        

	CANNON CONCRETE PRODUCTS LTD.

TONROE, ORANMORE, CO. GALWAY IRELAND
EIRCODE H91 H6W2
                                                              14

                                                      EN 771-3:2011+ A1:2015

Intended use: Common masonry unit for use as external walls, or as internal walls, in load bearing or non-loading building and civil engineering applications.

	Category 11                              L x W x H = 440mm X 215mm X 100mm aggregate 

	Dimensions:                              length 440mm, width 99mm, height 215mm

	Dimensions tolerances:             
                                    Category                              D1

                                    Flatness                                +3mm; -5mm

                                    Plane Parallelism                 +3mm; -5mm           

	Compressive strength: mean                                    8.8 N/mm2

	Dimensional stability: moisture movement
                  Mean moisture expansion coefficient of the masonry units is 0.28mm/m

                  Mean drying shrinkage coefficient of the masonry units is 0.13mm/m

                  Mean expansion coefficient of the masonry units is 0.15mm/m

	Shear bond strength:                                                NPD

	Flexural bond strength:                                            NPD

	Reaction to fire:                                                        A1

	Water absorption:                                                     3.2 g/(m2s)

	Water vapour diffusion coefficient:                         NPD

	Direct airborne sound insulation:
                                     Mean Gross dry density                1900 kg/m3

                                     Configuration                                as above

	Thermal conductivity:                                              0.95 (W/mK)

	Durability against freeze–thaw                               not to be left exposed

	Dangerous substances:                                             NPD


