[image: image1.png]



DECLARATION OF PERFORMANCE (DOP):
Cannon Concrete Products Ltd, 006 
Oranhill,

Oranmore,

Co Galway







18
IS EN 12620:2002 + SR16 2004 

Aggregates for Concrete
4/20, Gc80/20 (20mmAggs)
	Particle Shape
	Category
	FL18

	Particle Size
	Designation
	10/4,Gc80/20

	Particle Density
	Declared Value
	2.72 (Mg/m3)

	Water Absorption
	Declared Value
	0.4%

	Resistance to fragmentation
	Category
	LA20

	Sulphate Content (Acid Soluble)
	Category
	AS<0.1%

	Total Sulfar
	Category
	 S0.1

	Water Soluble Chloride  
	
	<0.001%

	Aggregate Abrasion Value
	Category
	AAV11

	Polished Stone Value
	Category
	PSV42

	Drying Shrinkage
	Category
	0.014%


