DECLARATION OF PERFORMANCE
Category 1 Aggregate Concrete Masonry Unit – Standard Solid 005
	 SSSS
	Code
	Name
	Actual Size
	Approx
Weight
KG
	Number
Per
Ton
	Number
Per
Pack
	Normal
Strength
N/mm2

	
	
	
	Length
	Height
	 Width
	
	
	
	

	[image: image1.png]



	104
	100mm Standard 7.5N
	440
	215
	100
	19
	52
	44
	7.5

	
	10004
	100mm Fair faced 7.5N
	440
	215
	100
	20
	50
	44
	7.5

	
	105
	100mm 13N
	440
	215
	100
	20
	50
	44
	13

	
	1004
	100mm 24N
	440
	215
	100
	20
	50
	44
	24

	
	106
	150mm Standard 7.5N
	445
	215
	140
	26
	38
	32
	7.5

	[image: image2.png]



	204
	L Block
	440
	210
	100
----
165
	21
	47
	16
	7.5

	[image: image3.png]



	201
	100mm Soap Bars
	435
	100
	100
	9
	110
	88
	7.5

	
	202
	150mm Soap Bars
	435
	140
	100
	13
	76
	66
	7.5

	
	206
	Stock Brick
	  210
	   65
	 100
	    3
	 333
	  128
	   7.5

	
	112
	300mm Cavity Closers
	  430
	 300
	 100
	    28
	 35
	   33
	   7.5

	[image: image4.png]



	109
	225mm Cavity Block
	430
	215
	215
	24
	41
	20
	4.5


1.
Unique identification code of the product type:

2.
Type, batch or serial number or any other element allowing identification of the construction product as required under Article 11(4) of the CPR:

Production details can be traced via dispatch docket.

3.
Intended use or uses of the construction product, in accordance with the applicable harmonized technical specification, as foreseen by the manufacturer:
I.S. EN 771-3 2001 Aggregate Concrete Masonry Units(Dense and Lightweight) intended for use as common, facing or rendered/protected exposed masonry in load bearing or non-loading building and civil engineering applications in accordance with Irish Building Regulations, TGD in particular parts A,B,C,D,E & L, Eurocode and SR 325.
4.
Name, registered trade name or registered trade mark and contact address of the manufacturer as required under Article 11(5):
CANNON CONCRETE PRODUCTS LTD.

TONROE, 
ORANMORE, 
CO. GALWAY 
IRELAND

H91 H6W2

5.
Authorised Representative: 
Not applicable

6.
System or systems of assessment and verification of constancy of performance of the construction product as set out in CPR, Annex V: 

AVCP System 2+

7.
Notified certification body:
NSAI (identification No. 050; FPC Cert No. 0050-CPR- 0224) performed the initial inspection of the manufacturing plant and of the factory production control and the continuous surveillance, assessment and evaluation of factory production control, and issued the certificate on constancy of conformity of the factory production control.
8.
Declared performance:                
	Characteristic
	Declared performance:                                   
	Technical Specification

	Dimensions tolerances:             
	D1  (+3MM, -5MM)
	I.S. EN 772-16

	Configuration
	Category 1 to EN 1996-1-1 Group 1                               
	EN 1996-1-1

	Dimensions:        L x W x H = 440mm X 215mm X 100mm aggregate                      
	length 438mm, width 98mm, height 214mm
	

	Compressive strength: mean
	9.8 N/mm2
	I.S. EN 772-11(7.3.2)

	Gross density 

(Direct Airborne Sound Insulation)
	>1900 kg/m3
	I.S. EN 772-13

	Net density 

(Direct Airborne Sound Insulation)
	>1900 kg/m3
	I.S. EN 772-13

	Dimensional stability: moisture movement

                  
	Mean moisture expansion coefficient of the masonry units is 0.22mm/m

                  Mean drying shrinkage coefficient of the masonry units is 0.2mm/m

                  Mean expansion coefficient of the masonry units is 0.42mm/m
Mean Moisture Content is 2%
	I.S. EN 772-14


	Shear bond strength:
	NPD
	I.S. EN 998-2

	Flexural bond strength:
	NPD
	I.S. EN 998-2

	Reaction to fire:
	Class A1
	Based on Commission Decision 200/605 EC amending 96/603 EC
(Refer to I.S. EN 1996-1-2 National Annex Table NA. 3.1/3.2 and 3.3 for fire rations of wall constructed with Class A1 Units)

	Water absorption:
	16.4 g/(m2s)
	

	Water vapour diffusion coefficient:
	NPD
	

	Thermal conductivity:
	0.95 (W/Mk)

	To ASTM-D 5334-22a

	Thermal resistivity
	1.06 (Km/W)
	To ASTM-D 5334-22a

	Durability against freeze–thaw                               

                                                                                   
	not to be left exposed
Suitable for use in:

Masonry condition Situations A1and A2 as outlined in Table 12 of S.R. 325:2013=A2:2018.

(Work below or near external ground level) – MX2.1/2.2 

 Net density
	

	Dangerous substances:
	NPD
	


9. The performance of the product identified in points 1 and 2 is in conformity with the declared performance in point 8. The declaration of performance is issued under the sole responsibility of Cannon Concrete Products Ltd. 
Signed for on behalf of the manufacturer by:

Cathal Melia, Quality Control Technician, Cannon Concrete Products Ltd:

05/03/26




Cathal Melia
