[image: image1.png]



DECLARATION OF PERFORMANCE (DOP):
Cannon Concrete Products Ltd, 002
Oranhill,

Oranmore,

Co Galway







18
IS EN 13242 &  Aggregates for unbound & hydraulically bound materials.

SR 21

Granular Fill to Annex E of SR 21: 2014 & A1 2016; suitable 




For use under concrete floors & footpaths.
T.1 STRUC 0/31.5mm GA80
	Essential Characteristics 
	Performance 
	Clause 
	Test Method

	Geometrical
	0/31.5
	Table E.2
	IS EN 933-1

	Fines Content
	F7
	Table E.2
	IS EN 933-1

	Water Absorption
	WA242.72 (Mg/m3)
	5.4.2
	IS EN 1097-6

	Magnesium Sulphate
	MS253
	5.4.
	IS EN 1367-2

	Resistance to fragmentation
	LA20
	5.2.2.1
	IS EN 1097-2

	Sulphate Content (Acid Soluble)
	AS0.1
	5.11
	IS EN 13242:2002 + A1:2007

	Total Sulfar
	S0.1
	5.8
	IS EN 13242:2002 + A1:2007

	Plasticity Index
	Liquid Limits 20
	5.4.1
	BS 1377- Part 2


