[image: image1.png]



DECLARATION OF PERFORMANCE (DOP):
Cannon Concrete Products Ltd, 004
Oranhill,

Oranmore,

Co Galway







18

IS EN 13242 &  
Aggregates for unbound & hydraulically bound materials.

SR 21

Granular Fill to Annex E of SR 21: 2014 & A1 2016; suitable 




For use under concrete floors & footpaths.

IS EN 12620:2002 + SR16 2004 Aggregates for Concrete

T.3 BLIND 0/4 GF85/Quarry Dust
	Essential Characteristics 
	Performance 
	Clause 
	Test Method

	Geometrical
	0/4
	Table 4
	IS EN 933-1

	Fines Content
	F16
	Table E.3
	IS EN 933-1

	Resistance to fragmentation
	LA25
	5.2.2.1
	IS EN 1097-2

	Sulphate Content (Acid Soluble)
	AS0.1
	5.11
	IS EN 13242:2002 + A1:2007

	Total Sulfar
	S0.1
	5.8
	IS EN 13242:2002 + A1:2007


	Sieve Size mm
	FPC tolerance
	Conformity Specification % passing 

	8
	100
	100

	6.3
	99
	98-100

	4
	80
	80-99


